| „DŽEMAL BIJEDIĆ“ UNIVERSITY OF MOSTAR FACULTY OF MECHANICAL ENGINEERING |
| --- |
| Course name: | Welding metallurgy | Course code: 0000 |
| Cycle level, year, semester | Master's degree | 2nd. academic year. / autumn |
| Course teacher: | Full prof. Sead Pašić |
| Contact: | Room: O008 E-mail: sead.pasic@unmo.ba Tel.:+38736571258 |
| Student workload in hours: | Lectures weekly: 2 hours | Excercises weekly: 2 hours | Total: (30+30) |
| Number of ECTS credits: | ECTS: 6 |
| Base qualification: | Mechanical engineering |
| Course status: | Mandatory |
| Preconditions for Course: | - |
| Limitations for Course: | None |
| ECTS explanation: |  |
| Course goal: | Goal of this course is to understand all processes and changes that are present in material during welding, with aim to issue most suitable welding technology of different steels. |
| Description of the general and speciffic competences (knowledge and skills) / learning outcomes: | After completition of this course, students are going to be able to calculate all thermical processes during the welding process, to predict structural and mechanical charateristics of welds and HAZ and to prescribe most suitable welding technology . Also, they would be able to test weldability of some carbon steels. |
| Course contents: | Introduction to welding metallurgy Physical characteristics of welding Thermical characteristics of welding, heat exchange with environment, heat conductivity, heat fields. Thermical cycle of welding, cooling speed and time during the welding proccess Welding metallurgy basics, conditions of occurrence of weld pool and its characteristics, reaction of liquid metal on environmental gases. Pre-heating Structural transformations during welding proccess Weldability of steel Testing of weldability Warm cracks Cold cracks Lamelar splitting Cracks caused by annealing |
| Form of teaching: | Lectures, auditory excercises and laboratory excercises |
| Other student obligations: |  |
| Items of Assesment: | Two partial tests during semester (7th and 15th week). Final exam in 16th week. Grade: Attendance – 5%. Partial tests – 20%+20% = 40% Term paper – 25% Final exam – 30% |
| Base literature and references: | O.Pašić: „Zavarivanje“, Svjetlost Sarajevo 1999. I. Hrivnjak, „Zavarljivost čelika“, Građevinska knjiga, Beograd, 1982. V. Semjan, LJ. Katnić, A. Imamović, Ž. Petrović, „Teorija zavarljivosti čelika“, Energoinvest IZE, Sarajevo, 1989. H. Granjon, „Werkstoffkundliche Grundlagen des Schweissens“, Dusseldorf 1993. |
| Course quality measurement: | Anonymous survey |